[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

Steel plate for for Boiler Pressure Vessel ASTM A 537class 1 steel
A 537class 1 steel plate, ASTM A 537class 1 steel plates is a kind of material for boiler and pressure vessel steel. ASTM A 537class 1 steel plates is characterized by a minimum yield strength of 280-355 MPa and by good weldability, so A 537class 1 steel is mainly used to for manufacturing boilers, pressure vessels and pipes transporting hot liquids. the following are ASTM A 537class 1 steel plate's Chemical composition and mechanical properties.

Chemical analysis -% by mass* (max) of A 537class 1 steel
	Grade
	C. %
	Mn.%
	S. 
	N
	Cu
	Nb
	Ti.
	Si.
	P. 
	AL
	Cr.
	Mo.
	Ni
	Vi

	A 537class 1
	0.10-0.22
	0.10-1.70
	0.015
	0.012
	0.30
	0.020
	0.03
	0.60
	0.025
	0.020
	0.30
	0.08
	0.30
	0.02



Mechanical properties of A 537class 1 steel
 

	Grade
	Type
	Thickness mm
	Yield strength Mpa(min)
	Tensile Strength  MPa
	Elongation % (min)
	Impact Energy (KVJ) (min)

	
	
	
	
	
	
	-20°
	0°
	+20

	A 537class 1
	Normalized
	≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250
	355
	510-650
	20
	27
	34
	40

	
	
	
	345
	510-650
	20
	27
	34
	40

	
	
	
	335
	460-580
	20
	27
	34
	40

	
	
	
	315
	490-630
	20
	27
	34
	40

	
	
	
	295
	480-630
	20
	27
	34
	40

	
	
	
	280
	470-630
	20
	27
	34
	40


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                          Web:http://www.shipbuilding-steel.com
Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.


