Steel Resistant to Atmospherical Corrosion steel plate

Steel Resistant to Atmospherical Corrosion steel information INCLUDEPICTURE "http://www.bebonchina.com/steel/img/pdf.gif" \* MERGEFORMATINET 


PDF
[image: image1.png]


WORDSteel Resistant to Atmospherical Corrosion steel information

BEBON steel is Steel Resistant to Atmospherical Corrosion steel supplier,we have much experience in manufacture Steel Resistant to Atmospherical Corrosion steel, We could give the fastest delivery time on the base of our competitive price directly from our mill. if you need know steel grade feature,we can provide Steel Resistant to Atmospherical Corrosion chemical composition and Steel Resistant to Atmospherical Corrosion mechanical properties.

[image: image2.jpg]


 [image: image3.jpg]


 [image: image4.jpg]



Resistant to Atmospherical Corrosion Steel also can be called weathering resistant steel or Atmospheric corrosion resistant structural quality steel . The steel for resistant to Atmospherical Corrosion is stronger & tougher than carbon steel,and is ductile, highly formable & weldable. High-strength low-alloy structural steel features atmospheric corrosion resistance, which is crucial in structural applications.Atmospheric corrosion resistant steel plate is mainly used to build containers ,truck frames, brackets, crane booms, rail cars and other comparable applications. 
The main grade of Resistant to Atmospherical Corrosion Steel are :
Material #: 1.8961, 1.8945, 1.8946, 1.8959,1.8963 , 1.8965, 1.8966, 1.8967
EN 10155 : S 235 J0WP, S 235 J2WP, S 235 J2W,S 355 J0W, S 355 J2G 1W, S 355 J2G2W, S 355 K2G1W, S 366K2G2W
WBL 087: WSt 37-2 , W St 37-3 ,W St 52-3 
NFA 35502 : E 24W 2 , E 24 W 3 , E 24 W 4 , E 36 WB 3 , E 36 WB 4, E 36 WA 3,E 36 WA 4
BS 4360:WR 50 A, WR 50 B,WR 50 C
CSA G 4021:gr 350 -A AT,gr 400-A AT
ASTM:A242 gr1, A 600 A/B/C, A588grA, A709gr50W
Fe 235W  Fe 355 W
SMA50AW--SMA50CP
UNI: Fe 360 DK 1, Fe 510 C1K1, Fe 510 D1K1, Fe 510 C2K1, Fe 510 D2K1

 

	Material #
	EN 10155
	SEW 087
	NFA 35-502
	UNI
	BS 4360
	UNE
	ASTM
	JIS G3114

	1.8961
	S235J2W
	WTSt 37-3
	E 24 W 4
	Fe 360 DK 1
	　
	　
	　
	　

	1.8945
	S355J0WP
	　
	E 36 WA 3
	Fe 510 C1K1
	WR 50 A
	　
	　
	　

	1.8946
	S355J2WP
	　
	E 36 WA 4
	Fe 510 D1K1
	　
	　
	A 242 Type 1
	　

	1.8959
	S355J0W
	　
	E 36 WB 3
	Fe 510 C2K1
	WR 50 B
	　
	A 588 - A 242 Gr. 1
	SMA 50 AW

	1.8963
	S355J2G1W
	WTSt 52-3
	　
	Fe 510 D2K1
	WR 50 C
	　
	A 588 Gr. A
	　

	1.8965
	S355J2G2W
	　
	　
	　
	　
	　
	　
	SMA 50 CP

	1.8966
	S355K2G1W
	　
	E 36 WB 4
	　
	　
	　
	A 709 Gr. 50 W
	　

	1.8967
	S355K2G2W
	　
	　
	　
	　
	　
	　
	　



If you need to buy Steel Resistant to Atmospherical Corrosion steel, we will strictly according to the customer put forward the specifications of the Steel Resistant to Atmospherical Corrosion, chemical composition, performance requirements such as supply goods,if you anything pls contact us. 

Source:http://www.bebonchina.com / steel / Product / Steel-Resistant-to-Atmospherical-Corrosion.html 

