Weldable normalized fine grained pressure vessel steels steel plate


BEBON steel is Weldable normalized fine grained pressure vessel steels steel supplier,we have much experience in manufacture Weldable normalized fine grained pressure vessel steels steel, We could give the fastest delivery time on the base of our competitive price directly from our mill. if you need know steel grade feature,we can provide Weldable normalized fine grained pressure vessel steels chemical composition and Weldable normalized fine grained pressure vessel steels mechanical properties.


 INCLUDEPICTURE "http://www.bebonchina.com/steel/uploadfile/201106/14/21101559841.jpg" \* MERGEFORMATINET 


  [image: image2.jpg]



Weldable normalized fine grained pressure vessel steels are characterised by a minimum yield strength of 275 - 460 MPa, by good weldability and high resistance to brittle cracking. Weldable normalized fine grained pressure vessel steels are used above all for manufacturing vessels for pressurised gas (LPG, butane and propane tanks), pressure vessels, steam boiler parts, pressure piping, compressors etc.The following special grades are available for extraordinary applications:
P...NL1 and P...NL2 or P...ML1 and P...ML2 for application temperatures below -20 °C;
P...NH for operating temperatures of up to 400 °C.
The user of these Weldable normalized fine grained pressure vessel steels must make sure that his calculation, design and processing methods are appropriate for the material. The welding technique used must be suitable for the intended application .
The main grade of  Weldable normalized fine grained pressure vessel steels are :
Material #: 1.0486, 1.0487, 1.0488, 1.1104, 1.0562, 1.0565, 1.0566, 1.1106. 
EN 10028-3: P275N,P275NH , P275NL1, P275NL2, P355N, P355NH, P355NL1, P355NL2.
DIN 17102: StE 285, WStE 285, TStE 285, EStE 285, StE 355, WSteE 355, TStE 355, EStE 355.
NFA 36-207 : A 510 AP, A 510 AP, A 510 FP 1.
UNI 7382 : Fe E 355 KG, Fe E 355-2, Fe E 355-3. 
BS 1501: 224 Gr. 400, 224 Gr. 430, 223 Gr. 490, 224 Gr. 490, 225Gr. 490
UNE 36081: AE 355 KG
ASTM: A 516 Gr. 60, A 662 Gr. A, A 537 CL 1, A 662 Gr. C, A 737 Gr. B
 

	Material #
	EN 10028-3
	DIN 17102
	NFA 36-207
	UNI 7382
	BS 1501
	UNE 36081
	ASTM

	1.0486
	P275N
	StE 285
	　
	　
	224 Gr. 400
	　
	　

	1.0487
	P275NH
	WStE 285
	　
	　
	224 Gr. 430
	　
	A 516 Gr. 60

	1.0488
	P275NL1
	TStE 285
	　
	　
	　
	　
	A 662 Gr. A

	1.1104
	P275NL2
	EStE 285
	　
	　
	　
	　
	　

	1.0562
	P355N
	StE 355
	A 510 AP
	Fe E 355 KG
	223 Gr. 490
	AE 355 KG
	A 537 CL 1

	1.0565
	P355NH
	WSteE 355
	A 510 AP
	Fe E 355-2
	224 Gr. 490
	　
	A 662 Gr. C

	1.0566
	P355NL1
	TStE 355
	A 510 FP 1
	Fe E 355-3
	224 Gr. 490
	　
	A 737 Gr. B

	1.1106
	P355NL2
	EStE 355
	　
	　
	　
	　
	　



If you need to buy Weldable normalized fine grained pressure vessel steels steel, we will strictly according to the customer put forward the specifications of the Weldable normalized fine grained pressure vessel steels, chemical composition, performance requirements such as supply goods,if you anything pls contact us. 

Source:http://www.bebonchina.com / steel / Product / Weldable-normalized-fine-grained-pressure-vessel-steels.html 

Tags: P275N, P275NH , P275NL1
ABS AH32 ABS AH36 ABS AH40 ABS DH32 S460NL TStE460 ABS DH36 ABS DH40 ABS EH32 TStE285
