[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

 The  EN 10028-2 10CrMo9-10 steel plate/sheet,Application of Pressure vessel &Boiler 10CrMo9-10 steel plate/sheet: widely used in petroleum, chemical, power station boilers making and other industries for the production of reactor, heat exchanger, separator, spherical tanks, oil cans, gas cans, nuclear reactor pressure vessel, boiler steam package, liquefied petroleum gas cylinders, high pressure water main station, hydraulic turbine vortex shells and other equipments and components;High-strength & low-alloy 10CrMo9-10  steel plate: widely used in plants building, general mansions and all kinds of construction machinery, such as mines and various types of drilling rig used in construction, power shovel, electric wheel dump trucks, mining vehicles, excavators, loaders, bulldozers , various types of cranes, hydraulic support, coal mining machinery and equipments and other structures.

	   


10CrMo910 EN 10028-2Number:1.7380
	Comparision of steel grades

	
	DIN 17155
	10 CrMo 9 10

	
	NFA 36-205
	10 CD 9.10

	
	UNI 5869
	-

	
	BS 1501
	622 Gr.31

	
	UNE 36087
	-

	
	ASTM
	A 387 Gr.22

	
	JIS G3115
	-


10CrMo9-10 steel plate Chemical Composition [%]

	Grade
	C.  
	Mn.  
	S.  
	N
	Cu
	Nb
	Ti.  
	Si.
	P.  
	AL.
	Cr.
	Mo.
	Ni.
	V.

	10CrMo910
	0.08-0.14
	0.40-0.80
	0.010
	0.012
	0.30
	-
	-
	0.50
	0.020
	-
	2.00-2.50
	0.90-1.10
	-
	-



10CrMo9-10 steel sheet Mechnical Properties
	Grade
	Thickness mm
	Yield strength Mpa
	Tensile Strength  MPa
	Elongation (A) %
	Impact Energy KV at Test temperature [J]

	
	
	
	
	
	-20°
	0°
	+20

	    13CrMo 4-5
	≤16
	310
	480-630
	18
	-
	-
	31

	
	16>to≤40
	300
	480-630
	18
	 
	 
	31

	
	40>to≤60
	290
	480-630
	18
	-
	-
	31

	
	60>to≤100
	280
	470-620
	17
	-
	-
	27

	
	100>to≤150
	265
	460-610
	17
	-
	-
	27

	
	150>to≤250
	250
	450-600
	17
	-
	-
	27


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


