[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10028 16M03steel plate/sheet for boiler steels
16MO3 steel plate/sheet, EN10028 16MO3 steel plate/sheet, under EN10028 standard, we can regard 16MO3 steel plate/sheetfor boiler steels.
16MO3 steel plate/sheet is one mainly of Steel for boiler steels.EN10028 16MO3 steel is mainly used for boilers and pressure vessels with elevated temperatures equivalent to DIN17155 15Mo3 and UNI5869 15Mo3, 15D3 (NFA 36205 ) and ASTM A204Gr.B.
 

	    16Mo3 EN 10028-2Number:1.5415
	Comparision of steel grades

	
	DIN 17155
	15 Mo 3

	
	NFA 36-205
	15 D3

	
	UNI 5869
	15 Mo 3

	
	BS 1501
	1503 - 243 B

	
	UNE 36087
	16 Mo 3

	
	ASTM
	A 204 Gr. B

	
	JIS G3115
	-



16Mo3  steel plate Chemical Composition
 

	Grade
	C. max
	Mn.  
	S.  
	N
	Cu
	Si.
	P.
	Cr.
	Ni.
	Mo.

	16Mo3
	0.12- 0.2
	0.40- 0.90
	0.01
	0.012
	0.30
	0.35
	0.025
	0.30
	0.30
	0.25- 0.35


16Mo3  steel sheetMerchanical Propertites 
 

	Grade
	Tensile Strength (Mpa)
	Yield Strength (Mpa)
	Elongation in 100-150 mm(%)
	Elongation in 16 mm(%)
	Max Thickness (mm)

	16Mo3
	440-590
	220-275
	19
	24
	250


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


