[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

SM520B/C steel plate, JIS3106  SM520B/C steel plate, under JIS3106 standard, we can regard  SM520B/C steel plate as Carbon and low alloy steel  SM520B/C steel plateis one mainly of Carbon and low alloy steel,  SM520B/C steel grade is a low carbon, high strength structural steel With this low carbon equivalent, it process good cold forming property. SM520B steel platesusual supplied in normalized or control rolled delivery condition

	    50EE BS4360  
	Comparision of steel grades

	
	CSAG40-21
	-

	
	IS
	-

	
	JIS 3101
	-

	
	JIS 3106
	SM 520 B

	
	ISO 630
	-

	
	ASTM
	-



50EE  steel plate Chemical Composition
 

	Grade
	Chemical Composition, [%]

	
	C. max
	Si.
	Mn. max
	P. max
	S.
	Nb.
	V.
	Normal supply Condition (1),(2)

	50EE
	0.18
	0.10- 0.50
	1.50
	0.040
	0.030
	0.003-0.10
	0.003-0.10
	Normalized


50EE  steel  sheet Mechnical Properties 
	Grade
	Minimun charpy V-notch impact Test value
	Minimum elongation,A, On a gauge length[1]
	Mimimun yield strength,Re, For thickness (in mm) [2] N/m㎡
	Tensile StrengthRm[1] N/m㎡ [6]

	
	Thickness mm [5]
	Energy Min. [J]value
	Temp. ℃
	80mm [3]
	200mm [4]
	5.65 √So
	≤16
	16-40
	40-63
	63-100
	100-150
	

	50EE
	75(10)
	27
	-50
	20%
	18%
	20%
	355
	345
	340
	325
	305
	480/640(8)(9)


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


