[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

ASTM A516Gr60 steel plate/sheet,ASTM A516Gr60 steel plate/sheet, under ASTM standard, we can regard A516Gr60 steel plate/sheetfor simple pressure vessels steel.

ASME SA516Gr60 is a boiler and pressure vessel quality steel which is ideal for moderate and lower temperature service.The material is used extensively by industrial boiler and pressure vessel fabricators who provide manufacturing support to the oil, gas and petrochemical industry. The steel has good weldability and excellent notch toughness.

Chemical Composition of ASTM A516 Gr60/ASME SA516Gr60
 

	Carbon(C)
	%
	Manganese(Mn)
	%
	Phosphorus(P)
	%

	12.55mm or less
12.5-50mm
50-100mm
100-200mm
>200mm
	0.21
0.23
0.25
0.27
0.27
	12.5mm or less
Heat Analysis
Product Analysis
Over 12.5mm
Heat Analysis
Product Analysis
	  0.6-0.9
0.55-0.98 0.85-1.20
0.79-1.30
	   
(max)
	    0.035

	Sulphur(S)
	%
	Silicon(Si)
	%
	 

	(max)
	0.035
	Heat Analysis
Product Analysis
	0.15-0.40
0.13-0.45
	


Mechanical Properties of ASTM A516Gr60/ASTM SA516Gr60

	Description
	Grade60

	Tensile Strength(Ksi)
Tensile Strength(MPa)
Yield Strength(Ksi)
Elongation in 200mm(min.%)
Elongation in 50mm(min.%)
Thickness(max/min)
	60-80
415-550
32
220
21
25
205


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


