[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

SS490 steel plate, JIS3101 SS490 steel plate, under JIS3101 standard, we can regard SS490 steel plate as Carbon and low alloy steel SS490 steel plate is one mainly of Carbon and low alloy steel, SS490 steel plate is alloy steel under the EN standard which is equal to DIN17100:St52-3,EN10025:S355JR,BS:50B and UNI7070:Fe510B 
 

	　
　
　
　
A656
ISO 630

Number:1.0557

　
　
　
　
	Comparision of steel grades

	
	EN 10025(93)
	S 355 J2G4

	
	EN 10025(90)
	FE 510 D D1

	
	EN 10113-2
	S355NL

	
	JIS 3106
	SS 490 YA

	
	ASTM
	A 656 Gr 50


A656 steel plate Chemical analysis -% by  mass*
	Grade
	C≤ 16mm

max
	C>16mm

max
	Si

max
	Mn

max
	P

max.
	S

max.

	A656
	0.2
	0.2
	0.55
	1.6
	0.035
	0.035


A656 steel sheet Mechanical properties
	Grade
	Thickness
	Yield Strength
	Tensile Strength
	Fracture
	Notch impact

	
	(mm)
	ReH[N/mm2]
	Rm [N/mm2]
	Elongation
	Energy1)Ch Vcomplete

	
	　
	Transv.min
	Transv.
	[%]transv.min
	Sample longitude

	
	　
	　
	　
	　
	Min[J]

	　
　
　
　
A656

　
　
　
　
	T≤16
	355
	-
	-
	　

	
	T>16
	345
	-
	-
	　

	
	T<3
	-
	510-680
	-
	　

	
	T≥3
	-
	490-630
	-
	-20 degree

	
	Up to 1.5
	-
	-
	13
	27J

	
	1.50-2.00
	-
	-
	14
	　

	
	2.01-2.50
	-
	-
	15
	　

	
	2.51-2.99
	-
	-
	16
	　

	
	≥3
	-
	-
	20
	　


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


