[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

ABS DH36 steel plate,ABS DH36 steel sheet,ABS Grade DH36 shipbuilding steel price,ABS Grade DH36 steel supplier and manufacturer.

ABS DH36 Shipbuilding Steel Description:

All ABS steels are standard carbon steels. All of these steels have been engineered to be optimal long-lived shipbuilding steels.As with other grades of steel, they have a specific gravity of 7.8.Higher-strength ABS shipbuilding steel comes in six grades of two strengths, The ABS DH36 grades have yield strength of 51,000 psi (355 MPa), and ultimate tensile strength of 71,000 - 90,000 psi (490-620 MPa).

ABS DH36 Shipbuilding Steel Application:

ABS DH36 Shipbuilding steel plates are suitable for container and bulk cargo vessels as well as cruise ships, ferries and yachts. 

ABS DH36 Steel Grade Specification:

Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm

Length: 3000mm to 18000mm. 

ABS DH36 Ship Steel Delivery Conditions: 
ABS DH36 Delivery Condition: AR(As hot rolled only), TMCP, Q+T(Quenching+Tempering), N(Normalizing),CR( Control rolled only)

ABS DH36 Steel Plate Additional Service: 

Hot rolled(HR), control rolled(CR) Thermo Mechanical Control Process(TMCP), Normalized , Q&T, impact test, Z15,Z25,Z35.

ABS DH36 Shipbuilding Steel Chemical Composition:

	Grade
	C %
	Si %
	Mn %
	P %
	S %
	V %
	AL %
	Cr %

	ABS Grade DH36
	0.180
	0.1-0.5
	0.90-1.6
	0.035
	0.035
	0.05-0.10
	0.015
	0.200

	
	Cu %
	Mo %
	Nb %
	Ni %
	Ti %
	 
	 
	 

	
	0.350
	0.080
	0.02-0.05
	0.400
	0.020
	 
	 
	 


ABS DH36 Grade Ship Steel Mechanical Properties:   

	Grade
	Thickness(mm)
	MinYield(Mpa)
	Tensile(Mpa)
	Elongation (%)
	Min Impact Energy

	ABS Grade DH36
	8mm-50mm
	Min 355Mpa
	490-620Mpa
	21%
	-20
	34J

	
	51mm-70mm
	Min 355Mpa
	490-620Mpa
	21%
	-20
	41J

	
	71mm-100mm
	Min 355Mpa
	490-620Mpa
	21%
	-20
	50J

	The min impact energy is longitudinal energy


BEBON ABS DH36 shipbuilding steel plates and sheets have been exported to worldwide shipyard and ship building company,we have mill ABS Grade DH36 for shipbuilding.If you have any needs in ABS Grade DH36 steel plate price and suppliers, please feel free to contact us.
[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

