[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

ABS EH40 steel plate,ABS EH40 steel sheet,ABS Grade EH40 shipbuilding steel price,ABS Grade EH40 steel supplier and manufacturer.

ABS EH40 shipbuilding Steel Description:

All ABS EH40 steels are standard carbon steels. All of these steels have been engineered to be optimal long-lived shipbuilding steels.

ABS EH40 Shipbuilding Steel Application:

ABS EH40 Shipbuilding steel plates are suitable for container and bulk cargo vessels as well as cruise ships, ferries and yachts. 

ABS EH40 Steel Grade Specification:

Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm

Length: 3000mm to 18000mm. 

ABS EH40 Ship Steel Delivery Conditions: 
ABS EH40 Delivery Condition: AR(As hot rolled only), TMCP, Q+T(Quenching+Tempering), N(Normalizing),CR( Control rolled only)

ABS EH40 Steel Plate Additional Service: 

Hot rolled(HR), control rolled(CR) Thermo Mechanical Control Process(TMCP), Normalized , Q&T, impact test, Z15,Z25,Z35.

ABS EH40 Shipbuilding Steel Chemical Composition:

	Grade
	C %
	Si %
	Mn %
	P %
	S %
	V %
	AL %
	Cr %

	ABS Grade EH40
	0.180
	0.1-0.5
	0.90-1.6
	0.035
	0.035
	0.05-0.10
	0.015
	0.200

	
	Cu %
	Mo %
	Nb %
	Ni %
	Ti %
	 
	 
	 

	
	0.350
	0.080
	0.02-0.05
	0.400
	0.020
	 
	 
	 


ABS EH40 Grade Ship Steel Mechanical Properties:   

	Grade
	Thickness(mm)
	MinYield(Mpa)
	Tensile(Mpa)
	Elongation (%)
	Min Impact Energy

	ABS Grade EH40
	8mm-50mm
	Min 390Mpa
	510-650Mpa
	20%
	-40
	34J

	
	51mm-70mm
	Min390Mpa
	510-650Mpa
	20%
	-40
	41J

	
	71mm-100mm
	Min 390Mpa
	510-650Mpa
	20%
	-40
	50J

	The min impact energy is longitudinal energy


BEBON ABS EH40 shipbuilding steel plates and sheets have been exported to worldwide shipyard and ship building company,we have mill ABS Grade EH40 for shipbuilding.If you have any needs in ABS Grade EH40 steel plate price and suppliers, please feel free to contact us.

[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

