[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

ABS Grade D shipbuilding steel plate,ABS D marine steel plate, Grade D steel plate for ship building,ABS D ship steel sheet supplier.

ABS Grade D Shipbuilding Steel Description:

ABS Steels are types of structural steel which are standardized by the American Bureau of Shipping for use in shipbuilding.ABS steels come many grades in ordinary-strength and two levels of higher-strength specifications.

ABS Grade D shipbuilding Steel Application:
ABS D grades of steel plate are almost exclusively used in the Shipbuilding Industry for the construction of structural parts of ships, barges and marine equipment. These grades are certified by ABS – American Bureau of Shipping.

ABS Grade D Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm

Length: 3000mm to 18000mm. 

ABS D Ship Steel Delivery Conditions: 
ABS D Delivery Condition: AR(As hot rolled only), TMCP, Q+T(Quenching+Tempering), N(Normalizing),CR( Control rolled only)

ABS Grade D Steel Plate Additional Service: 

Hot rolled(HR), control rolled(CR) Thermo Mechanical Control Process(TMCP), Normalized , Q&T, impact test, Z15,Z25,Z35.

ABS Grade D Shipbuilding Steel Chemical Composition Heat Analysis:

	Element
	ABS Grade D  Max %
	Element
	ABS Grade D  max %

	C
	0.21
	Ni
	- 

	Mn
	0.60
	Mo
	 -

	Si
	0.1-0.35
	Al
	 -

	S
	0.035
	 Nb
	- 

	P
	0.035
	V
	- 

	Cu
	- 
	Ti
	-

	Cr
	 -
	N
	- 


ABS Grade D Ship Steel Mechanical Properties:    

	Grade
	Thickness
	Yield Strength
	Tensile Strength
	Elongation
	Impact Energy

	
	(mm)
	MPa (min)
	MPa
	% (min)
	(KV J) (min)

	
	 
	 
	 
	 
	-20 degree

	ABS Grade D
	4-260
	235
	400-520
	22
	27J


Note: the impact energy under less 50mm thickness
BEBON ABS Grade Specification:ABS marine steel plate D, ABS marine vessel used steel plates, Steel Plate ABS Grade D shipbuilding steel plate, ABS Grade D specification,ABS Grade D sheet, ABS Grade D shipping building steel plate.
[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

