[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

EN10250 C55 steel, steel plates,C55 steel sheet, is a kind of high carbon steel plates,steel sheets in EN10250 standard. The following are EN10250 C55 steel chemical composition and mechanical properties. If you want to know C55 steel price , please contact us-- bebon international. We are the professional C55 supplier.

	C55 EN 10250-2:1999, Number: 1.0535
	 
	Comparison of steel grades

	
	
	JUS
	Č.1630

	
	
	DIN
	C55

	
	
	BS
	070M55

	
	
	GOST
	55

	
	
	AISI
	1055

	
	
	UNI
	C55

	
	
	NF
	(AF70C55), IC55


 Chemical analysis -% by mass
	Chemical elements
	C
	Si 
max.
	Mn
	P max.
	S
max.
	Cr
max.
	Mo
max.
	Ni
max.
	Cr+Mo+Ni
max.
	 

	%, by mass
	0,52-0,60
	0,40
	0,60-0,90
	0,045
	0,045
	0,40
	0,10
	0,40
	0,63
	-

	Permissible deviation
	±  0,02
	+ 0,03
	± 0,04
	+ 0,005
	+ 0,005
	+ 0,05
	+ 0,03
	+ 0,05
	 
	-


At the option of the manufacturer the elements aluminium, titanium, vanadium and niobium may be added singly or in combination for  grain size control purposes. Elements not quoted in table shall not be added  to the steel without the agreement of  the purchaser, except for the purpose  of  finishing the heat.   
Mechanical properties in the normalized and normalized and tempered conditions

	Thickness of ruling section tR

	Diameter in mm
	tR ≤ 100mm
	100< tR ≤250mm
	250< tR ≤500mm
	500< tR ≤1000mm

	Re min  (N/mm2)
	330
	330
	260
	250

	Rm min (N/mm2)
	640
	620
	600
	590

	A % min.
	l-longitudinal
	12
	12
	12
	11

	
	tr -transverse
	-
	9
	9
	8

	KV min * (J)
	l-longitudinal
	-
	-
	-
	-

	
	tr -transverse
	-
	-
	-
	-


1N/mm2=1MPa Maksimim hardness for forgings to be supplied in the annealed condition

	HB max 229


Heat treatment conditions 

	  Quenching Temperature, 0C  
	Cooling medium
	Tempering Temperature, 0C
	Normalizing  
temperature, 0C

	805 to 845
	Oil or water
	550 to 660
	825 to 865


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 www.bebonchina.com,                                           Skype：bebonchina
www.shipbuilding-steel.com
www.steel-plate-sheet.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.                       

