[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

Carbon structural and high strength low alloy steel

Common carbon structural steel also be called Mild steel. This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. Carbon structural steel usually be rolled into steel plates, shaped steel and profile steel, which usually used to build workshop,bridge,vessels and so on .The delivery station usually are hot rolled,control rolled, or Normalized 

.

The main grade of common carbon structural steel are : 

EN10025(93):S185,S235JR,S235J0,S235J2,S235J2G3,S235J2G4,

EN10025(90): Fe310-0,Fe E360B,Fe E360C,Fe E360D1,Fe E360D2,

DIN17100: St33,St37-2,St37-3U,St37-3N

ASTM:A283GrA/B/C/D,A284GrC/D,A36,

JIS3101:SS330,SS400,SS490

JIS3106:SM400A/B/C

Low alloy high strength steel also can be called common low alloy steel,low alloy structural steel. Low alloy structural steel's total alloy content usually is not more then 3% .Except for Si and Mn, there is V,Ti,Nb,Al,Cr,Ni,Re,N and so on.

The main steel grades in Carbon and low alloy steel are like : 

EN10025(93):S355JR,S355J0,S355J2,S355J2G3,S355J2G4,S355K2G3,S355K2G4,S275JR,S275J0,S275J2,S275J2G3,S275J2G4.

EN10025(90): Fe430B,Fe430C,             

Fe430D1,Fe430D2,Fe510B,Fe510C,Fe510D1,Fe510D2,Fe510 D D1,Fe510 D D2.

EN10113-2: S275N,S275NL,S355N,S355NL

DIN17100: St44-2,St44-3U,St44-3N,St52-3,St52-3N.

JIS3101:SS330,SS400,SS490

JIS3106:,SM490A/B/C,SM490YA/B,SM520B/C

ASTM:A529Gr42/50,A572Gr42/50,A573Gr58/65/70,A633GrA/C/D,A656Gr50,A709Gr36/50/50w/A808.

ISO630: FE 310, FE 360B/C/D, FE 430B/C/D , FE 510B/C/D , A656

	Europe
	Germany
	Canada
	India
	Japan
	International
	USA

	EN10025 (93)
	EN10025 (90)
	EN10113-2
	DIN 17100
	CSAG40-21
	IS
	JIS3101
	JIS 3106        
	ISO 630
	ASTM

	S185
	Fe 310-0
	
	St 33
	
	
	SS 330
	
	
	

	
	
	
	
	
	
	
	
	FE 310
	

	S235JR(G2)
	Fe E360B(FN)
	
	RSt 37-2
	230 G
	IS226
	SS400
	SM 400A
	Fe 360 B
	A 36/A283C

	S235 J0
	Fe E 360 C
	
	St37-3U
	
	Fe 410-S
	
	SM400B
	Fe 360C
	

	S235J2G3
	Fe E 360 D1
	
	St 37-3 N
	
	
	
	SM400C
	Fe 360 D
	

	S235J2G4
	FeE360 D2
	
	
	
	
	
	
	
	

	
	
	
	
	
	
	
	
	
	

	S275 JR
	Fe430 B
	
	ST 44-2
	260W,WT
	IS2062
	
	
	Fe 430B
	A529GR 42,50

	S 275 JO
	Fe 430 C
	
	St44-3U
	
	Fe410 WA
	
	
	Fe 430C
	

	S275 J2G3
	Fe430 D1
	S 275N
	St 44-3N
	
	Fe 410 WB
	
	
	Fe 430D
	

	
	
	
	
	
	
	
	
	
	

	S275 J2G4
	Fe430 D2
	S 275NL
	
	
	Fe 410 WC
	
	
	
	

	
	
	
	
	300W.WT
	
	
	
	
	

	
	
	
	
	
	
	
	
	
	

	
	
	
	
	
	
	
	
	
	

	
	
	
	
	
	
	
	
	
	

	S 355 JR
	Fe510 B
	
	
	350 W, WT
	IS 961
	SS490
	SM 490A
	FE 510 B
	A572gr,42,50

	S 355 JO
	 Fe 510 C
	
	St 52-3 U
	
	Fe 570 HT
	
	SS490B
	Fe 510 C
	

	Fe 510 D1
	
	
	
	
	
	
	
	
	

	S 335J2G4
	Fe 510 D2
	S 355 NL
	
	
	
	
	SS 490 YA
	A 656
	

	S 335K2G3
	Fe 510 D D1
	
	
	
	
	
	SS490 YB
	
	

	S 335K2G4
	Fe 510 D D2
	
	
	
	
	
	SM 520 B
	
	

	
	
	
	
	
	
	
	SM 520 C
	
	


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

