[image: image1.jpg]BEBON

BebonChina.com

3




[image: image2.jpg]


                                      Henan BEBON international co.,ltd

EN10111 DD11 steel,DD11 steel plates,DD11 steel sheet, is a kind of stamping and cold forming steel in EN10111 standard. The following are EN10111 DD11 steel chemical composition and mechanical properties. If you want to know DD11 steel price , please contact us-- bebon international. We are the professional DD11 supplier.

	DD11 EN 10111 Number: 1.0332
	Comparison of steel grades

	
	UNI5867
	FEP11

	
	DIN1614
	STW22

	
	NFA 36-301
	1C

	
	JIS G 3131
	SPHD

	
	ASTM-SAE
	A621DQ-SAE1010

	
	BS1449
	HR3

	
	UNE36.093
	AP11


 Chemical analysis -% by mass* 

	Chemical elements
	C
	Si 
max
	Mn max
	P
max.
	S
max.

	%,by mass
	0.12
	--
	0.60
	0.045
	0.045


 

 

 
Mechanical properties
	thickness
	Yield StrengthReH
[N/mm2] transv.min.
	TensileStrengthRm
[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	BendingTesttransv.
bendingmandrel 
Øangle = 180°s =
plate thickness

	t≤ 16mm t >16mm
	170-340
	 
	 
	1 S

	   t < 3mm 

   t ≥ 3mm
	 
	440
	 
	

	Up to 1.5mm 

1.51-2.00mm 

2.01-2.50mm 

2.51-2.99mm 

 ≥ 3mm
	 
	 
	  23 A80 24 A80   28 A5
	


 
[image: image2.jpg]Bebon steel  ——  The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 www.bebonchina.com,                                           Skype：bebonchina
www.shipbuilding-steel.com
www.steel-plate-sheet.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.                       

