[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

EN10111 DD14 steel,DD11 steel plates,DD14 steel sheet, is a kind of stamping and cold forming steel in EN10111 standard. The following are EN10111 DD14 steel chemical composition and mechanical properties. If you want to know DD14 steel price , please contact us-- bebon international. We are the professional DD14 supplier.

 

	DD14
 EN 10111 Number: 1.0389
	Comparison of steel grades

	
	UNI5867
	-

	
	BS1449
	-

	
	NFA 36-301
	3CT

	
	JIS G 3131
	-

	
	ASTM-SAE
	-

	
	UNE36.093
	-


Chemical analysis -% by mass*

	Chemical elements
	C
	Si 
max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.08
	--
	0.35
	0.025
	0.025


 




Mechanical properties 
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	BendingTesttransv.
bendingmandrel 
Øangle = 180°s = plate thickness
 

	t≤ 16mm
t >16mm
	170-3290
	 
	 
	0 S

	  t < 3mm
   t ≥ 3mm
	 
	380
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	 
31 A80
32 A80
 
36 A5 
	


 

[image: image2.jpg]


Bebon steel  ——  The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 www.bebonchina.com,                                           Skype：bebonchina
www.shipbuilding-steel.com
www.steel-plate-sheet.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.                       

