[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10025 E295 steel plate/sheet,EN10025 E295 steel plate/sheet, under EN standard, we can regard E295 steel plate/sheet for general Construction steels.EN10025 E295 steel plate/sheet is for general Construction steels.The followings are the chemical composition and the mechanical properties of EN E295 steel.

	E295
DIN EN 10025-2Number: 1.0050
	Comparison of steel grades

	
	EN10025:1990
	FE 490-2

	
	DIN17100
	ST50-2

	
	NFA 35-501
	A50-2

	
	BS1449
	-

	
	UNI7070
	FE 490


E295 steel plate Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm

max
	C>16mm

max
	Si
max
	Mn

max
	P
max.
	S
max.
	N

max

	%,by mass
	-
	-
	-
	-
	0.045
	0.045
	0.012


E295 steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]

transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact

Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm

t >16mm
	295

285
	 
	 
	-

-

	   t < 3mm

  t ≥ 3mm
	 
	490-600

470-610
	 
	

	Up to 1.5mm

1.51-2.00mm

2.01-2.50mm

2.51-2.99mm

 ≥ 3mm
	 
	 
	11

12

13

14

18
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


