[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

DIN EN 10025-2  E335 steel plate/sheet  is one kind General Construction Steel plates , E335 steel  is a Pure steel, micro-alloying with good mechanical properties and weldability; high strength, stable yield strength , and has a low rate of tensile strengthand yield strength

	E335
DIN EN 10025-2Number: 1.0060
	Comparison of steel grades

	
	EN10025:1990
	FE 590-2

	
	DIN17100
	ST60-2

	
	NFA 35-501
	A60-2

	
	BS1449
	-

	
	UNI7070
	FE 590


E335 steel plate Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.
	N
max

	%,by mass
	-
	-
	-
	-
	0.045
	0.045
	0.012


E335 steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	335
325
	 
	 
	-
-

	   t < 3mm
  t≥ 3mm
	 
	590-770
570-710
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	7
8
9
10
14
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


