[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10025 E360 steel plate/sheet,EN10025 E360 steel plate/sheet, under EN standard, we can regard E360 steel plate/sheet for general Construction steels.EN10025 E360 steel plate/sheet isfor general Construction steels.The followings are the chemical composition and the mechanical properties of EN E360 steel.E360 steelis according to EN10025 standard and it is equivalent to EN:Fe690-2,DIN17100:St70-2,NFA: A70-2 and UNI7070:Fe690 steel grades.

	E360
DIN EN 10025-2Number: 1.0070
	Comparison of steel grades

	
	EN10025:1990
	FE 690-2

	
	DIN17100
	ST70-2

	
	NFA 35-501
	A70-2

	
	BS1449
	-

	
	UNI7070
	FE 690


E360 steel sheet Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.
	N
max

	%,by mass
	-
	-
	-
	-
	0.045
	0.045
	0.012


E360 steel plate Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	360
355
	 
	 
	-
-

	   t < 3mm
  t≥ 3mm
	 
	690-900
670-830
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	4
5
6
7
10
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


