[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10025 E360 steel plate/sheet,EN10025 E360 steel plate/sheet, under EN standard, we can regard E360 steel

plate/sheet for general Construction steels.EN10025 E360 steel plate/sheet is for general Construction steels.The

followings are the chemical composition and the mechanical properties of EN E360 steel.E360 steel is according to

EN10025 standard and it is equivalent to EN:Fe690-2,DIN17100:St70-2,NFA: A70-2 and UNI7070:Fe690 steel grades.

	EH36
 
	Comparison of steel grades

	
	Norske Veritas
	NVE36

	
	Germanischer Lloyds
	E36

	
	Bureau Veritas
	EH36

	
	American Bureau of Shipping
	EH36

	
	USSR Register
	E 36

	
	Nippon Kaigi Kyoka
	-


EH36 steel sheetChemical analysis-% by  mass*

	 Grades
Material number
	C

max
	Si max
	Mn.

max
	P

max
	S

max
	N

max
	AL

min
	Cr max
	Cu max
	Mo max
	Ni max
	Nb

max
	Ti

 max
	V

max

	EH36
	0.20
	0.60
	0.90

-1.60
	-
	0.035
	-
	0.015-0.06
	0.2
	0.35
	0.08
	0.5
	0.02

-0.05
	0.04
	0.05

-0.10


 EH36 steel plate Mechanical  properties
	Grades
	Yield Strength

ReH[N/mm2]

transv.min.

　
	Tensile

Strength

Rm[N/mm2]transv.

　
	Fracture

Elongation

[%]transv. min.

　
	　Impact bending test

	
	
	
	
	Thickness

mm
	Test temperature

°C
	Impact work, KV,

J, min

	EH36
	　

 355

　
	　

   490 - 620

　
	　

    21

　
	5.5 – 7.0
	-40
	      24

	
	
	
	
	7.5 – 9.5
	 -20
	      38

	
	
	
	
	≥10
	   0
	      34


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


