[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

Fine-grain structural steels

The fine-grain structural steel grades are characterised by a minimum yield strength of 275 - 460 MPa, by good weldability and high resistance to brittle cracking. Fine-grain structural steels are used above all for manufacturing vessels for pressurised gas (LPG, butane and propane tanks), pressure vessels, steam boiler parts, pressure piping, compressors etc. 


Main grades of Fine-grain structural steels are :
Material #: 1.8818, 1.8819, 1.8823, 1.8834, 1.8825, 1.8836, 1.8827, 1.8838.
EN 10113-3: S275M, S275ML, S355M, S355ML, S420M, S420ML, S460M, S460ML.
SEW 083: StE 275 TM, TStE 275 TM, StE 355 TM, TStE 355 TM, StE 420 TM, TStE 420 TM, StE 460 TM, TStE 460 TM.
NFA 36-201: E 355 R, E 355 FP, E 420 R, E 420 FP, E 460 R, E 460 FP.
UNI 7382: Fe E 275 KGTM, Fe E 275 KTTM, Fe E 355 KGTM, Fe E 355 KTTM, Fe E 460 KGTM, Fe E 460 KGTM.
BS 4360: 50 EE, 55 EE.
ASTM: A 572 Gr. C, A 633 Gr. C, A 572 Gr. 60, A 633 Gr. E, A 572 Gr. 65 
Material # : 1.049,  1.0491,  1.0545 , 1.0546,  1.8902,  1.8912
EN 10111: S275N, S275NL, S355N, S355NL,  S420N, S420NL, 
DIN 1614/2: StE 285, TStE 285, StE 3555, TStE 355, StE 420, TStE 420, 
NFA 36-301: E 355 R, E 355 FP, E 420 R, E 420 FP
UNI 5867: Fe E 275 KGN, Fe E 275 KTN, Fe E 355 KGN, Fe E 355 KTN, Fe E 420 KGN. 
BS 1449 : 43 EE, 50 E, 50 EE, 50 F 
UNE 36.093 : AE 355 KG , AE 355 KT, AE 420 KG
ASTM : A 572 Gr. 42,  A 633 Gr. A,   A 572 Gr. 50   A 633 Gr. C/D ,  A 537 CI. 1     A 255 Gr. D    A 633 Gr. E / A 572 Gr. 60 / A 738 Gr. C
JIS G3131: SM490A

	Material #
	EN 10111
	DIN 1614/2
	NFA 36-301
	UNI 5867
	BS 1449
	ASTM - SAE

	1.049
	S275N
	StE 285
	　
	Fe E 275 KGN
	　
	A 572 Gr. 42

	1.0491
	S275NL
	TStE 285
	　
	Fe E 275 KTN
	43 EE
	A 633 Gr. A

	1.0545
	S355N
	StE 355
	E 355 R
	Fe E 355 KGN
	50 E
	A 572 Gr. 50

	1.0546
	S355NL
	TStE 355
	E 355 FP
	Fe E 355 KTN
	50 EE
	A 633 Gr. C, D / A 537 CI. 1

	1.8902
	S420N
	StE 420
	E 420 R
	Fe E 420 KGN
	　
	A 255 Gr. D

	1.8912
	S420NL
	TStE 420
	E 420 FP
	　
	50 F
	A 633 Gr. E / 
A 572 Gr. 60 / 
A 738 Gr. C

	Material #
	EN 10113-3
	SEW 083
	NFA 36-201
	UNI 7382
	BS 4360
	ASTM

	1.8818
	S275M
	StE 275 TM
	　
	Fe E 275 KGTM
	　
	　

	1.8819
	S275ML
	TStE 275 TM
	　
	Fe E 275 KTTM
	　
	　

	1.8823
	S355M
	StE 355 TM
	E 355 R
	Fe E 355 KGTM
	　
	A 572 Gr. C

	1.8834
	S355ML
	TStE 355 TM
	E 355 FP
	Fe E 355 KTTM
	50 EE
	A 633 Gr. C

	1.8825
	S420M
	StE 420 TM
	E 420 R
	　
	　
	A 572 Gr. 60

	1.8836
	S420ML
	TStE 420 TM
	E 420 FP
	　
	　
	A 633 Gr. E

	1.8827
	S460M
	StE 460 TM
	E 460 R
	Fe E 460 KGTM
	　
	A 572 Gr. 65

	1.8838
	S460ML
	TStE 460 TM
	E 460 FP
	Fe E 460 KGTM
	55 EE
	A 572 Gr. 65


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

