[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

General purpose structural steels

General purpose structural steel is same with common carbon structural and high strength low alloy steel actually .  Just the former us called by it’s application, the later by it’s Elements and performance.

General purpose structural steel is usually used for commercial & industrial building structure: pre-engineered buildings, pre-fabricated buildings, warehouses, car parks, workshops, sports stadiums. Structural steel plates for multi-storey steel frame structures, airport hangars, railway stations structure, shopping malls etc.. High strength low alloy heavy plates for bridge construction. Plate steel for construction of railway & road vehicle chassis.

The main steel grades of General purpose structural steel plates are:
Material #: 1.0035, 1.0037, 1.0038, 1.0116, 1.0117, 1.0044, 1.0143, 1.0144, 1.0145, 1.0045, 1.0553, 1.057, 1.0577, 1.0595,1.0596, 1.005, 1.006, 1.007
EN 10025: S185, S235JR, S235JRG2,S235J2G3, S235J2G4, S275JR, S275JO, S275J2G3, S275J2G4, S355JR, S355JO, S355J2G3, S355J2G4, S355K2G3, S355K2G4, E295, E335, E360
DIN 17100: St 33, St 37-2, RSt 37-2, St 37-3 N, St 44-2, St 44-3 U, St 44-3 N, St 52-3 U, St 52-3 N, St 50-2, St 60-2, St 70-2.
ASTM: A 283 B - A 569 CQ, A 283 C - A 570 Gr. 33, A 283 D - A 36, A 578 Gr. 70, A 633 Gr. A, A 572 Gr. 50 - A 678 Gr. A, A 441. 
JIS G3101: SS 330, SS 400, SS 490, SS 500.

	Material #
	EN 10025
	DIN 17100
	NFA 35-501
	UNI 7070
	BS 4360
	UNE 36.080
	ASTM
	JIS G3101

	1.0035
	S185
	St 33
	A 33
	Fe 320
	
	A 310-0
	A 283 B - A 569 CQ
	SS 330

	1.0037
	S235JR
	St 37-2
	E 24-2
	Fe 360 B
	40 A
	
	A 283 C - A 570 Gr. 33
	

	1.0038
	S235JRG2
	RSt 37-2
	E 24-2 NE
	
	40 B
	AE 235 B-FN
	
	

	1.0116
	S235J2G3
	St 37-3 N
	E 24-4
	Fe 360 D
	40 D
	AE 235 D
	
	

	1.0117
	S235J2G4
	
	
	
	
	
	
	

	1.0044
	S275JR
	St 44-2
	E 28-2
	Fe 430 B
	43 B
	AE 275 B
	A 283 D - A 36
	SS 400

	1.0143
	S275JO
	St 44-3 U
	E 28-3
	Fe 430 C
	43 C
	AE 275 C
	A 578 Gr. 70
	

	1.0144
	S275J2G3
	St 44-3 N
	E 28-4
	Fe 430 D
	43 D
	AE 275 D
	A 633 Gr. A
	

	1.0145
	S275J2G4
	
	
	
	
	
	
	

	1.0045
	S355JR
	
	E 36-2
	Fe 510 B
	50 B
	AE 355 B
	A 572 Gr. 50 - A 678 Gr. A
	SS 490

	1.0553
	S355JO
	St 52-3 U
	E 36-3
	Fe 510 C
	50 C
	AE 355 C
	A 441
	

	1.057
	S355J2G3
	St 52-3 N
	
	Fe 510 D
	50 D
	AE 355 D
	
	

	1.0577
	S355J2G4
	
	
	
	
	
	
	

	1.0595
	S355K2G3
	
	E 36-4
	
	50 DD
	
	
	

	1.0596
	S355K2G4
	
	
	
	
	
	
	

	1.005
	E295
	St 50-2
	A 50-2
	Fe 490
	
	A 490
	
	SS 500

	1.006
	E335
	St 60-2
	A 60-2
	Fe 590
	
	A 590
	
	

	1.007
	E360
	St 70-2
	A 70-2
	Fe 690
	
	A 690
	
	


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

