[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

High Yield strength steel

High Yield strength Steel means the steel grades are characterised by a minimum yield strength of 380 to 700 N/mm2, by good weldability and high resistance to brittle cracking.

Most the high yield steel type are steel bar. And high yield strength steel can be used many industrial area: like wear-resistant steel, boiler and pressure vessel steel, and so on.

The main steel grades of High Yield strength steel are :

EN 10028-3:P 460 N, P 460 NH, P 460 NL1, P 460 NL2

DIN 17102:STE 380 , WSt E 380 ,T St E 380 ,E St E 380 ,STE 420, WSt E 420, T St E 420, E St E 420, STE460, WSt E 460 ,T St E 460, E St E 460 .

NFA 36201:E 375R,E 375 FP,E 420R,E420 FP,E460R,E 460 FP.

NFA 35207:A 550 AP, FP      A 590 AP, FP      AE 410 DD

MNC 810E:SS21,42,01   SS 21,44,01    SS 21,45,01   SS 26,52, 00    SS 26,54,11  

BS 4360:55 C, EE

CSA G40-21: 400 W, WT

JIS 3101:SS 540, (3116) SPV 450, (3106) SM 570

ASTM: A 572Gr60/65 , A633GrE, A656Gr60/70/80.

	Europe
	Germany
	France
	Japan
	USA

	EN 10028-3
	 DIN 17102
	NFA 36201
	NFA 35207
	
	JIS 3101
	ASTM

	
	STE 380
	E 375R
	
	
	SS 540
	A 572gr. 60,65

	
	
	
	
	
	
	

	
	WSt E 380
	E 375 FP
	
	
	
	

	
	T St E 380
	
	
	
	
	

	
	E St E 380
	
	
	
	
	A 633grade E

	
	
	
	A 550 AP, FP
	AE 410 DD
	
	

	
	St E 420
	E 420 R
	
	
	
	

	
	W St E 420
	E 420 FP
	
	
	
	

	
	T St E 420
	
	
	
	
	

	
	E St E 420
	
	
	
	
	

	
	
	
	A 590 AP, FP
	
	(3116)SPV 450
	A 656gr 60,70,80

	P 460 N
	St E 460
	E 460 R 
	
	
	(3106) SM 570
	

	P 460 NH
	W St E 460
	E 460 FP
	
	
	
	

	P 460 NL1
	T St E 460
	
	
	
	
	

	P 460 NL 2
	E St E 460
	
	
	
	
	


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

