[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

API 5L X80 steel plate/pipes for large diameter pipes X80 steel plate/pipes, API 5L X80 steel plate/pipes, under API 5L standard, we can regard X80 steel plate/pipes as large diameter pipes.

X80 steel plate/pipes is one mainly of Steel for large diameter pipes,API-X80 steel with good low temperature toughness was developed and the buckling behavior of X80 steel plate/pipe was investigated through large scale deformation tester. 

	L555MB
 EN10208-2   Material#1.8978
	Comparison of steel grades

	
	API5L
	   X80


L-555MBX-80 steel plateChemical analysis -% by  mass*

	Grades
	Material number
	C

max
	Si max
	Mn.

max
	P

max
	S

max
	AL

min
	Mo max
	Ni max
	Nb max

	L555MB
	1.8978
	0.08
	0.26
	1.75
	0.011
	0.0005
	0.03
	0.27
	0.22
	0.070


L-555MBX-80 steel sheetMechanical Propertities
	 Grade
	 Permissible yield point
ratio 
	 Yield Strength
MPa(min)
	 Tensile Strength
MPa
	 Elongation
% (min)

	 L555MB
	  ≤ 0.90
	    555
	 625 - 700
	    20


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


