[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

NK E36 Shipbuilding steel plate

The NK E36 steel plate is the mainly kinds of steel for shipbuilding and oil platform, the shipbuilding grade NK E36 can be used in the manufacture of the ship's hull structure, whose weight is more then 10000 tons. Shipbuilding grade NK E36 Steel is the high tensile strength steel,  NK E36 steel for shipbuilding and oil platform must be good toughness properties, higher strength, strong corrosion-resistance, the processing properties, and welding properties.

NK E36 steel plate Chemical Composition %
	
Grade
	C max
	Si max
	Mn
	P max
	S max
	Als min
	Ti max
	Cu max
	Cr
max
	Ni
max
	Mo
max
	Nb
	V

	NK E36
	0.18
	0.50
	0.90-1.60
	0.035
	0.035
	0.015
	0.02
	0.35
	0.20
	0.40
	0.08
	0.02-0.05
	0.05-0.10


Note: Generally speaking CE will be ≤ 0.40%. If the delivery condition is TMPC, the CE will be : ≤ 0.38% (thickness ≤ 50mm),≤0.40%( when the thickness >50-100).
Ceq% =(C+Mn)/6+(Cr+Mo+V)/5+(Ni+Cu)/15.
NK E36 steel plate Mechanical Property
	
Grade
	Rm
(MPa)
	Re(MPa) min
	A% min
	Akv/J min

	NK E36
	490-630
	355
	21
	E.T °C
	Thickness (mm)

	
	
	
	
	-40
	≤ 50
	>50-70
	>70-100

	
	
	
	
	
	L
	C
	L
	C
	L
	C

	
	
	
	
	
	34
	24
	41
	27
	50
	34


Note: In the list , Rm: .tensile strength,Re: Yield strength,A%: elongation, E.T: experimental temperature,L: lengthways, C: crosswise.
NK E36 steel plate Condition Of Delivery
	
Grade
	Fine grains elements
	category
	The thickness of steel

	
	
	
	≤ 12
	>12.5-20
	>20-25
	>25-35
	>35-50
	>50-100

	NK E36
	Any
	Plate/sheet
	N,TM

	
	
	Profile steel
	N(25),TM(25),AR*(15),CR*(15)
	-


Note: 1. delivery condition: A =Any ; N=Normalized ; CR=Control Rolled ; TM=TMPC, Temperature - deformation control rolling; AR*= Can be hot rolled with the agreement of Classification Society ; CR*=Can be control rolled with the agreement of Classification Society .
2.  The Figure in the ( ) means the sampling volume to do the impact test, the unit is Ton.(-) means without impact test.

NK E36 steel Contrast in the different standard

	
ASTM A131M
	TOCT 5521
	BS LR
	GB712

	NK E36
	E36
	EH36
	E36


Key Words: Supply NK E36 steel for shipbuilding, NK E36 steel for shipbuilding manufacturer,

         NK E36 steel for shipbuilding suppliers, manufacture NK E36 steel for shipbuilding,

          NK E36 steel for shipbuilding warehouser,

[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

