[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10028 P275Nsteel plate/sheet,EN10028 P275N steel plate/sheet, under EN standard, we can regard P275N steel plate/sheet for boilers and Pressure Vessels steels.EN10028P275N steel plate/sheetis for boilers and Pressure Vessels steels,it is a normalized steel plate and sheetwhich is mainly used for building pressure vessels and boilers and pipes for hot liquid.

	P275NH
EN10028-3 MATERIAL#1.0487
	Comparison of steel grades

	
	UNE36081
	-

	
	DIN17102
	WStE 285

	
	NFA 36-207
	-

	
	BS1501
	224Gr.430

	
	ASTM
	A516Gr.60


    P275N steel sheetChemical   Composition
	Grades
	C

≤
	Si. ≤
	Mn.
	P

≤
	S

≤
	N

≤
	AL

≥
	Cr

≤
	Cu

≤
	Mo

≤
	Ni

≤
	Nb

≤
	Ti

≤
	V

≤

	P275NH
	0.16
	0.40
	0.80~1.50
	0.025
	0.015
	0.012
	0.020
	0.30
	0.30
	0.08
	0.50
	0.05
	0.03
	0.05


 P275N steel  plateMechanical Propertities
	Thickness

 
	Yield Strength

ReH[N/mm2]

transv.min
	Tensile

Strength

Rm[N/mm2]transv
	Fracture Elongation[%]transv. min.
	Notch Impact

Energy1)Ch Vcomplete samplelongitud. min [J]

	5﹤t≤150mm
	275
	430 to 530
	-
	-


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


