[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10028 P275NL2 steel plate/sheet,EN10028 P275NL2 steel plate/sheet, under EN standard, we can regard P275NL2 steel plate/sheetfor boilers and Pressure Vessels steels.EN10028 P275NL12 steel plate/sheetis for boilers and Pressure Vessels steels,it is a normalized steel plate and sheet which is mainly used for building pressure vessels and boilers and pipes for hot liquid.And the followings are the chemical composition and mechanical properties of P275NL2.

	EN 10028-2

P275NL2
	Comparison of steel grades

	
	DIN 17135
	       T St E 285

	
	NFA36205
	        -



P275NL2  steel plate Chemical analysis -% by  mass*

	Grades
	C

max
	Si max
	Mn.

max
	P

max
	S

max
	N

max
	AL

min
	Cr max
	Cu max
	Mo max
	Ni max
	Nb max
	Ti max
	V

max

	P275NL2
	0.16
	0.4
	0.80-1.50
	0.02
	0.01
	0.012
	0.02
	0.3
	0.3
	0.08
	0.5
	0.05
	0.03
	0.05



P275NL2  steel sheetMechanical properties
	Grade
	Thickness

(mm)

 
	Yield Strength
MPa(min)
	Tensile Strength

MPa
	Elongation

% (min)

	P275NL2

 
	
	
	
	

	
	≤16
	275
	390 to 510
	24

	
	16＜t ≤40
	265
	390 to 510
	24

	
	40＜t ≤60
	255
	390 to 510
	24

	
	6＜t ≤100
	235
	370 to 490
	23

	
	100＜t ≤150
	225
	360 to 480
	23

	
	150＜t ≤250
	215
	350 to 470
	23


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


