[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

EN10028 P355NH steel,P355NH steel plates,SPA-H steel sheet, is a kind of weldable normalized fine grained pressure vessel steel in EN10028 standard. The following are EN10028 P355NH steel chemical composition and mechanical properties. If you want to know P355NH steel price , please contact us-- bebon international. We are the professional P355NH supplier.

	P355NH
DIN EN 10028-3 Number:1.0565
	Comparison of steel grades

	
	ASTM
	A662 Gr. C

	
	DIN17102
	WsteE 355

	
	NFA 36-207
	A 510 AP

	
	BS1501
	224 Gr. 490

	
	UNI
	Fe E 355-2


Chemical analysis -% by mass*

	Chemical elements
	C
max
	Si 
max
	Mn
 
	P
max
	S
max.
	Cu
max
	Cr
 
	Ni
max
	V
max
	Nb
max
	Al
min

	%,by mass
	0.20
	0.50
	1.10-1.70
	0.025
	0.015
	0.30
	0.3-1.25
	0.50
	0.10
	0.05
	0.02


Mechanical properties 
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	355
345
	 
	 
	         +20   50J
           0   40J
         -20   30J
         -40    -
         -50    -

	   t < 3mm
   t ≥ 3mm
	 
	490-630
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	22
	


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 www.bebonchina.com,                                           Skype：bebonchina
www.shipbuilding-steel.com
www.steel-plate-sheet.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.                       

