[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

RINA EH32 shipbuilding steel plate; RINA EH32 shipbuilding sheet; RINA EH32 shipbuilding plate supplier; RINA EH32 shipbuilding plate price; RINA EH32 hull structure steel; RINA EH32 shipbuilding plate property.

3. RINA EH32 shipbuilding steel description

The EH32 steel plate/sheet is the mainly kinds of steel for shipbuilding and oil platform. Shipbuilding grade EH32 is the high tensile strength steel with good toughness properties, higher strength, strong corrosion-resistance, the processing properties, and welding properties. 

4. RINA EH32 shipbuilding steel Application range

As the super features, RINA EH32 steel plate/sheet can be used in the manufacture of the ship's hull structure, and usually do navigation around coastal and river area. Also, RINA EH32 shipbuilding steel is widely used in oil platform and offshore platform. 

5. RINA EH32 shipbuilding steel supply size

Thickness: 4mm-260mm
Width: 1200mm-4000mm
Length: 3000mm-18000mm
(other plate sizes and thicknesses are available on request )

4. RINA EH32 shipbuilding steel composition (%)

	
Grade
	C max
	Si max
	Mn
	P max
	S max
	Als min
	Ti max
	Cu max
	Cr
max
	Ni
max
	Mo
max

	EH32
	0.18
	0.50
	0.90-1.60
	0.035
	0.035
	0.015
	0.02
	0.35
	0.20
	0.40
	0.08


Note: Generally speaking CE will be ≤ 0.40%. If the delivery condition is TMPC, the CE will be : ≤ 0.36% (thickness ≤ 50mm), ≤0.38%( when the thickness >50-100). Ceq% =(C+Mn)/6+(Cr+Mo+V)/5+(Ni+Cu)/15. 
1. RINA EH32 shipbuilding steel mechanical property

	
Grade
	Rm
(MPa)
	Re(MPa) min
	A% min
	Akv/J min

	EH32
	440-570
	315
	22
	E.T °C
	Thickness (mm)

	
	
	
	
	-40
	≤ 50
	>50-70
	>70-100

	
	
	
	
	
	L
	C
	L
	C
	L
	C

	
	
	
	
	
	31
	22
	38
	26
	46
	31


Note: In the list , Rm: tensile strength, Re: Yield strength, A%: elongation, E.T: experimental temperature,L: lengthways, C: crosswise.  
6. RINA EH32 shipbuilding steel deliver condition
	
Grade
	Fine grains elements
	category
	The thickness of steel

	
	
	
	≤ 12
	>12.5-20
	>20-25
	>25-35
	>35-50
	>50-100

	EH32
	Any
	Plate/sheet
	N, TM

	
	
	Profile steel
	N(25),TM(25),AR*(15),CR*(15)
	-


Note: 1. delivery condition: A =Any; N=Normalized; CR=Control Rolled; TM=TMPC, Temperature - deformation control rolling; AR*= Can be hot rolled with the agreement of Classification Society ; CR*=Can be control rolled with the agreement of Classification Society.
2.  The Figure in the ( ) means the sampling volume to do the impact test, the unit is Ton.(-) means without impact test. 

We, Henan BEBON international is professional in exporting the steel for shipbuilding and oil platform, all kinds of shipbuilding steel plate are available with the certificate from the Classification Society. If you have any need of RINA EH32 shipbuilding steel, pls feel free to contact our sales-team, we will supply you RINA EH32 steel plate with the best quality, first class service, and competitive price.
[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

