[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

RINA EH36 shipbuilding steel plate; RINA EH36 shipbuilding sheet; RINA EH36 shipbuilding plate supplier; RINA EH36 shipbuilding plate price; RINA EH36 hull structure steel; RINA EH36 shipbuilding plate property.

1. RINA EH36 shipbuilding steel description

The EH36 steel plate is the mainly kinds of steel for shipbuilding and oil platform. the Shipbuilding grade EH36 is the high tensile strength steel, EH36 steel plate/sheet features are good toughness properties, higher strength, strong corrosion-resistance, the processing properties, and welding properties. 

2. RINA EH36 shipbuilding steel application arrange

RINA EH36 steel plate/sheet can be used in the manufacture of the ship's hull structure, and usually do navigation around coastal and river area. Also, RINA EH36 shipbuilding steel is widely used in oil platform and offshore platform. 

3. RINA EH36 shipbuilding steel supply size

Thickness: 4mm-260mm
Width: 1200mm-4000mm
Length: 3000mm-18000mm
(other plate sizes and thicknesses are available on request )

4. RINA EH36 shipbuilding steel composition (%)

	
Grade
	C max
	Si max
	Mn
	P max
	S max
	Als min
	Ti max
	Cu max
	Cr
max
	Ni
max
	Mo
max
	Nb
	V

	EH36
	0.18
	0.50
	0.90-1.60
	0.035
	0.035
	0.015
	0.02
	0.35
	0.20
	0.40
	0.08
	0.02-0.05
	0.05-0.10


Note: Generally speaking CE will be ≤ 0.40%. If the delivery condition is TMPC, the CE will be : ≤ 0.36% (thickness ≤ 50mm), ≤0.38%( when the thickness >50-100). Ceq% =(C+Mn)/6+(Cr+Mo+V)/5+(Ni+Cu)/15. 
3. RINA EH36 shipbuilding steel mechanical property

	
Grade
	Rm
(MPa)
	Re(MPa) min
	A% min
	Akv/J min


	EH36
	490-630
	355
	21
	E.T °C
	Thickness (mm)

	
	
	
	
	-40
	≤ 50
	>50-70
	>70-100

	
	
	
	
	
	L
	C
	L
	C
	L
	C

	
	
	
	
	
	34
	24
	41
	27
	50
	34


Note: In the list , Rm: tensile strength, Re: Yield strength, A%: elongation, E.T: experimental temperature,L: lengthways, C: crosswise.  
4. RINA EH36 shipbuilding steel deliver condition

	
Grade
	Fine grains elements
	category
	The thickness of steel

	
	
	
	≤ 12
	>12.5-20
	>20-25
	>25-35
	>35-50
	>50-100

	EH36
	Any
	Plate/sheet
	N,TM

	
	
	Profile steel
	N(25),TM(25),AR*(15),CR*(15)
	-


Note:1.delivery condition: A =Any; N=Normalized; CR=Control Rolled; TM=TMPC, Temperature - deformation control rolling; AR*= Can be hot rolled with the agreement of Classification Society ; CR*=Can be control rolled with the agreement of Classification Society.
2. The Figure in the ( ) means the sampling volume to do the impact test, the unit is Ton.(-) means without impact test. 
With the advanced productive technology and certification from the biggest eight Classification Society, Henan BEBON has became an outstanding exporter in steel plate, especial in RINA EH36 shipbuilding steel. More information about RINA EH36 shipbuilding steel plate, pls free to consult our sales-team. 
[image: image2.jpg]


Bebon steel  ——  The most professional exporter on weathering resistant steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                             Web:http://www.shipbuilding-steel.com

                                                               http://www.bebonchina.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.

