[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

S235J0 steel plate, EN10025 S235J0 steel plate, under EN10025 standard, we can regard S235J0 steel plateas Carbon and low alloy steel
S235J0 steel plate is one mainly of Carbon and low alloy steel, S235J0 steel plate would be used to built containers which can bear low temperature sea water. When customers order S235J0 steel plate from us,our mill should be roll them completely according to EN10025_2 specification, the mill would issue original Mill test certificates before taking delivery for checking

	S235J0
DIN EN 10025-2Number: 1.0114
	Comparison of steel grades

	
	EN10025:1990
	FE E 360 C

	
	DIN17100
	St37-3U

	
	NFA 35-501
	E24-3

	
	BS1449
	40C

	
	JIS3106
	SM400B

	
	UNI7070
	FE 360 C


S235J0 steel sheet Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.17
	0.17
	--
	1.40
	0.045
	0.045


S235J0 steel plate Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	235
225
	 
	 
	Degree: 0
AV: 27J

	   t < 3mm
  t≥ 3mm
	 
	360-510
340-470
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	16
17
18
19
24
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


