[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

EN10025 S235J2G4 steel,S235J2G4 steel plates,S235J2G4 steel sheet, is a kind of general purpose structural steel in EN10025 standard. The following are EN10025 S235J2G4 steel chemical composition and mechanical properties. If you want to know S235J2G4 steel price , please contact us-- bebon international. We are the professional S235J2G4 supplier.

	S235J2G4
DIN EN 10025-2Number: 1.0117
	Comparison of steel grades

	
	EN10025:1990
	FE 360 D2

	
	DIN17100
	-

	
	NFA 35-501
	-

	
	BS1449
	-

	
	UNI7070
	-


Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si 
max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.17
	0.17
	--
	1.40
	0.035
	0.035


Mechanical properties 
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	235
225
	 
	 
	Degree: -20
AV: 27J

	   t < 3mm
   t ≥ 3mm
	 
	360-510
340-470
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	16
17
18
19
24
	


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 www.bebonchina.com,                                           Skype：bebonchina
www.shipbuilding-steel.com
www.steel-plate-sheet.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.                       

