[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

SS400 steel plate, JIS3101 SS400 steel plate, under JIS3101 standard, we can regard SS400 steel plate as Carbon and low alloy steel SS400 steel plate is one mainly of Carbon and low alloy steel, SS400 steel platewould be used to built containers which can bear low temperature sea water.When customers order SS400 steel plate from us,our mill should be roll them completely according to JIS3101 specifications,the mill would issue original Mill test certificates before taking delivery for checking

SS400 steel plate Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.17
	0.20
	--
	1.40
	0.045
	0.045


SS400 steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	235
225
	 
	 
	20 degree
27J

	   t < 3mm
  t≥ 3mm
	 
	360-510
340-470
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	16
17
18
19
24
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


