[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

This is common carbon steel plate in S235JR, S235J0 and S235J2 steel grade. Heat analysis shall be used to determine the required chemical composition for carbon. Manganese, phosphorus, sulfur, silicon, and copper. Tensile strength, yield strength, and elongation shall be evaluated using tension test.
 
S symbol for structural steel
275 indication of the min specified yield strength for thickness of under 16mm.
JR symbol 20 temperature impact test.
J0 symbol 0 temperature impact test
J2 symbol -20 temperature impact test
S275JR, S275J0 and S275j2 steel is a structural steel grade which be used in riveted, bolted, or welded construction of bridges and buildings.
For more information of S275j0 steel, please refer them in followin

	S275J0
DIN EN 10025-2Number: 1.0143
	Comparison of steel grades

	
	EN10025:1990
	FE 430 C

	
	DIN17100
	ST44-3U

	
	NFA 35-501
	E28-3

	
	BS1449
	43C

	
	UNI7070
	FE 430 C


S275J0 steel plate Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.18
	0.18
	--
	1.50
	0.040
	0.040



S275J0 steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	275
265
	 
	 
	0 degree
27J

	   t < 3mm
  t≥ 3mm
	 
	430-580
410-560
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	13
14
15
16
20
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


