[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

DIN EN 10025-2  S275J2G3   steel plate/sheet  has very wide use. Because of the low Carbon content and without alloy element, carbon structural  S275J2G3   steel has the proper tensile strength, good toughness, plasticity,processing property. Carbon structural steel  S275J2G3   steel plate usually be rolled into steel plates, shaped steel and profile steel, which usually used to build workshop,bridge,vessels and so on .The delivery station usually are hot rolled,control rolled, or Normalized

	S275J2G3
DIN EN 10025-2Number: 1.0144
	Comparison of steel grades

	
	EN10025:1990
	FE 430 D1

	
	EN10113-2
	P275N

	
	DIN17100
	ST44-3N

	
	NFA 35-501
	E28-4

	
	BS1449
	43D

	
	UNI7070
	FE 430 D


S275J2G3 steel plate Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.18
	0.18
	--
	1.50
	0.035
	0.035


S275J2G3 steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	275
265
	 
	 
	-20 degree
27J

	   t < 3mm
  t≥ 3mm
	 
	430-580
410-560
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	13
14
15
16
20
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


