[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

S275N steel plate is under EN10025-3standard equivalent to DIN:StE285,which with a minimum impact energy of 20J at temperatures not lower than -20 degree and the tensile strength of S275N is 370 to 510MPa
s275nL steel plateis a hot rolled structural steels, which technical delivery conditions for normalized or normalized rolled in weldable fine grain structural

	S275J2G4
DIN EN 10025-2Number: 1.0145
	Comparison of steel grades

	
	EN10025:1990
	FE 430 D2

	
	DIN17100
	-

	
	NFA 35-501
	-

	
	BS1449
	-

	
	UNI7070
	-


S275J2G4 /S275NL steel plate   Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.18
	0.18
	--
	1.50
	0.035
	0.035


S275J2G4 /S275NL steel sheet   Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	275
265
	 
	 
	-20 degree
27J

	   t < 3mm
  t≥ 3mm
	 
	430-580
410-560
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	13
14
15
16
20
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


