[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

MATERIAL# 1.0490 S275N steel plate/sheet  is under EN10025-3 standard equivalent to DIN:StE285,

S275N steel plate/sheet  is  a minimum impact energy of 20J at temperatures not lower than -20 degree and the tensile strength of S275N is 370 to 510MPa

	S275N
 EN 10025-3 MATERIAL# 1.0490
	Comparison of steel grades

	
	UNE36081
	AE285KG/AE285KW

	
	DIN17102
	STE285

	
	NFA 36-207
	-

	
	UN
	Fe E 275KG N


S275N steel sheet Chemical analysis -% by mass*

	Chemical elements
	C
max
	Si
 max
	Mn
 
	P
max
	S
max.
	Cu
max
	Cr
max
	Ni
max
	V
max
	Nb
max
	Al
min

	%,by mass
	0.18
	0.40
	0.50-1.50
	0.030
	0.025
	0.55
	0.30
	0.30
	0.05
	0.05
	0.02



S275N steel plate Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	275
265
	 
	 
	         +20   KV 31J
           0   KV 27J
         -10    KV 24J
         -20    KV 20J
         -40    -
         -50    -

	   t < 3mm
  t≥ 3mm
	 
	370-510
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	24
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


