[image: image1.jpg]


Henan BEBON international co.,ltd.

[image: image3.jpg]


 

Structural steel plate S355J0 iscarbon_manganese steels with a guaranteed minimum yield strength and tensile strength,and
satisfactory ductility.Without any special rolling or heat treatment for S355J0 steel,The abbreviated designation of this
delivery condition shall be AR (As rolled).
Now we list the steel chemical composition and property as belows,customers should be foucsed on the values,else note
for long steel plate,the max S content can be increased for improved machinability by 0.010% by agreement if the steel is
treated to modify the sulphide morphology.

	S355J0
DIN EN 10025-2Number: 1.0553
	Comparison of steel grades

	
	EN10025:1990
	FE 510 C

	
	DIN17100
	ST52-3U

	
	NFA 35-501
	E36-3

	
	BS1449
	50C

	
	UNI7070
	FE 510 C


S355J0  steel plate Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.20
	0.20
	0.55
	1.60
	0.040
	0.040


S355J0  steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	355
345
	 
	 
	0 degree
27J

	   t < 3mm
  t≥ 3mm
	 
	510-680
490-630
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	13
14
15
16
20
	


[image: image2.jpg]BEBON

BebonChina.com

3




BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


