[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

S355J2G1W steel plate, EN 10155 S355J2G1W steel plate, under EN 10155 standard, we can regard S355 J2G1W steel plate as Steel Resistantto Atmospherical CorrosionS355J2G1W steel plateis one mainly of Steel Resistant to Atmospherical Corrosion, S355J2G1W steel plate is a weather-resistant structural steel with mechanical properties similar to S355J2G2. By adding Cr, Cu and Ni, it formed oxide layers stick firmly to the workpiece surface. This oxide layer prevents further corrosion of the steel.

	S355 J2G1W
       EN10155
	Comparison of steel grades

	
	EU 155
	Fe 510 D2K1

	
	WBL 087
	-

	
	NFA 35502
	E 36 WB 4

	
	BS4360
	WR 50 C

	
	CSA G 4021
	gr 400-A AT


 S355J2G1W steel sheet Chemical  Composition
	Grades
	C

max
	Si 
max
	Mn

 
	P
max
	S
max.
	Cu

max
	Cr

max
	Al

Min
	Ni

ma
	Mo

max
	Nb

 

	S 355 J2GW
	0.16
	0.50
	0.50-1.50
	0.035
	0.030
	0.25-0.55
	0.40-0.80
	0.02
	0.65
	0.30
	0.015-0.060


S355J2G1W steel plateMechanical Propertities
	Grades

 
	Yield Strength

ReH[N/mm2]

transv.min
	Tensile

Strength

Rm[N/mm2]trans
	Fracture Elongation[%]transv. min.
	Notch Impact

Energy1)Ch Vcomplete samplelongitud. min [J]

	S355J2G 1W
	355
	510 - 610
	22
	-


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


