[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10155S355J2WP steel plate/sheet, EN10155 S355J2WP steel plate/sheet, under EN standard, we can regard S355J2WP steel plate/sheetfor steel resistant to Atmospherical corrosion steels.

EN10155S355J2WP steel gradeis a hot rolled products of structural steels in technical delivery conditions with improved atmospheric corrosion resistance.The steel grade in S235 a maximum carbon equivalent value of 0.44% and for grade s355 a maximum carbon equivalent value of 0.52% based on the ladle analysis shall for all thickness.The followings are the chemical composition and mechanical properties of EN S355J2WP steel plate.

The chemical composition of EN S355J2WP steel plate,by max %
 

	Grade
	C
	Mn
	Cr
	Si
	N
	S
	Cu
	P

	S355
J2WP
	0.15
	1.1
	0.25-
1.35
	0.8
	0.01
	0.04-
0.035
	0.20-
0.60
	0.05-
0.16


The mechanical properties of EN S355J2WP steel plate

	Grade
	Yield Strength Min. [MPa]
Norminal Thickness (mm)
	Tensile Strength [MPa]
Norminal Thickness(mm)
	Impact
Degraa [J]

	S355
J2WP
	≤16
	>16
≤40
	>40
≤63
	>63
≤80
	>80
≤100
	>100
≤150
	≤3
	>3
≤100
	>100
≤150
	  -20
	  27

	
	355
	345
	-
	-
	-
	-
	510-680
	470-630
	-
	
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


