[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

Under DIN EN10025-2 standard Number: 1.0045 S355JR steel plate/sheet  is used to manufacture the plants of factory,the commonconstructure and construction machinery and equipment; for example:Drilling machine ,
Excavator,Tip lorry, Grab,Conweigh belt,Bulldozer ,all kinds of Chain Block, and other
machiney equipments.

	S355JR
DIN EN 10025-2Number: 1.0045
	Comparison of steel grades

	
	EN10025:1990
	FE 510 B

	
	DIN17100
	ST52-3

	
	ASTM
	A572GR50

	
	JIS
	SS490/SM490A

	
	NFA 35-501
	E36-2

	
	BS1449
	50B

	
	UNI7070
	FE 510 B


S355JR steel plate Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.24
	0.24
	0.55
	1.60
	0.045
	0.045


S355JR steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	355
345
	 
	 
	20 degree
27J

	   t < 3mm
  t≥ 3mm
	 
	510-680
490-630
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	13
14
15
16
20
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


