[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

S355K2G3 steel plate has a -20 degree temperature steel. Compare with S355J2 , S355K2 steel plate impact energy is 40J, S355J2 is 27J under 150mm thickness. So S355K2 steel plate is better for choice in low temperature high impact energy projects.
Bebon steel is specialized in supplying S355K2G3 steel grade in super thick steel plate. We exported our goods to Vietnam, Korea and Singapore in this grade in many years.Bebon steel promised that we used our best service to enlarge steel market of oversea.
If you need more yield and tensile strength, you could choose S450J0 steel gradeWhich has min 450Mpa yield strength.

	S355K2G3
DIN EN 10025-2Number: 1.0595
	Comparison of steel grades

	
	EN10025:1990
	FE 510 DD1

	
	DIN17100
	-

	
	NFA 35-501
	E36-4

	
	BS1449
	50DD

	
	UNI7070
	-


S355K2G3 steel plate Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm
max
	C>16mm
max
	Si
 max
	Mn
max
	P
max.
	S
max.

	%,by mass
	0.20
	0.20
	0.55
	1.60
	0.035
	0.035



S355K2G3 steel sheet Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	355
345
	 
	 
	-20 degree
40J

	   t < 3mm
  t≥ 3mm
	 
	510-680
490-630
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	13
14
15
16
20
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


