[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

EN10025 S355K2G4 steel,S355K2G4 steel plates,S355K2G4 steel sheet, is a kind of general purpose structural steel in EN10025 standard. The following are EN10025 S355K2G4 steel chemical composition and mechanical properties. If you want to know S355K2G4 steel price , please contact us-- bebon international. We are the professional S355K2G4 supplier.

	S355K2G4
DIN EN 10025-2Number: 1.0596
	Comparison of steel grades

	
	EN10025:1990
	FE 510 DD2

	
	DIN17100
	-

	
	NFA 35-501
	-

	
	BS1449
	-

	
	UNI7070
	-


Chemical analysis -% by mass*

	Chemical elements
	C≤ 16mm

max
	C>16mm

max
	Si 
max
	Mn

max
	P
max.
	S
max.

	%,by mass
	0.20
	0.20
	0.55
	1.60
	0.035
	0.035


Mechanical properties 
	thickness
	Yield StrengthReH[N/mm2]

transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact

Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm

t >16mm
	355

345
	 
	 
	-20 degree

40J

	   t < 3mm

   t ≥ 3mm
	 
	510-680

490-630
	 
	

	Up to 1.5mm

1.51-2.00mm

2.01-2.50mm

2.51-2.99mm

 ≥ 3mm
	 
	 
	13

14

15

16

20
	


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 www.bebonchina.com,                                           Skype：bebonchina
www.shipbuilding-steel.com
www.steel-plate-sheet.com 

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.                       

