[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

S355N steelis a structural steel grade. S means structural steel, 355 means min yield strength for thickness less 16mm expressed in Mpa, N mean the delivery condition.
 
Bebon steelcould provide max thickness to 350mm by using ingot. Max width 3800mm, we also could do the UT test, impact test, Chemical analysis, mechanical test, and Simulated may treatment according to our customer requirement.
About S355N steel detail information，please refer to technical date in following.

	S355N
 EN 10025-3 MATERIAL#1.0545
	Comparison of steel grades

	
	UNE36081
	AE355KG/AE355KW

	
	DIN17102
	STE355

	
	NFA 36-201
	E355R

	
	BS4036
	-

	
	UN
	Fe E 3555KG N


S355N  structural steelChemical analysis -% by mass*

	Chemical elements
	C
max
	Si
 max
	Mn
 
	P
max
	S
max.
	Cu
max
	Cr
max
	Ni
max
	V
max
	Nb
max
	Al
min

	%,by mass
	0.20
	0.50
	0.90-1.65
	0.030
	0.025
	0.55
	0.30
	0.50
	0.12
	0.05
	0.02



S355N  steel Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	355
345
	 
	 
	         +20   KV 31J
           0   KV 27J
         -10    KV 24J
         -20    KV 20J
         -40    -
         -50    -

	   t < 3mm
  t≥ 3mm
	 
	470-630
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	22
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


