[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

Normalized welded low alloy steel plate S420N,it shall be done low temperature charpy_V impacting test under EN10025 standard,the temperature shall be minus 20 centi degree,and the impacting energy shall be min 27J.

Now Bebon industrial list chemical composition and mechnical property for S420N steel plateas belows,for long
products the P and S content can be 0.005% higher than the values in the below sheet.Our mill also can offer customers the chemical composition limited specially by customers' requested.

	S420N
 EN 10111 MATERIAL#1.8902
	Comparison of steel grades

	
	UNE36081
	AE420KG/AE420KW

	
	DIN17102
	STE420

	
	NFA 36-201
	E420R

	
	BS4036
	-

	
	UN
	-



S420N steel plate Chemical composition -% by mass*

	Chemical elements
	C
max
	Si
 max
	Mn
 
	P
max
	S
max.
	Cu
max
	Cr
max
	Ni
max
	V
max
	Nb
max
	Al
min

	%,by mass
	0.20
	0.60
	1.00-1.70
	0.030
	0.025
	0.55
	0.30
	0.50
	0.12
	0.05
	0.02


S420N steel Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	420
400
	 
	 
	         +20   KV 31J
           0   KV 27J
         -10    KV 24J
         -20    KV 20J
         -40    -
         -50    -

	   t < 3mm
  t≥ 3mm
	 
	520-680
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	19
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


