[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10113 S460M steel plate/sheet,EN10113 S460M steel plate/sheet, under EN standard, we can regard S460M steel plate/sheetfor Fine-grain structural steels, thermomechanically rolled steel.

EN10113 S460M is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -20 degree

	  S460M EN 10113-3Number:1.8827
	Comparision of steel grades

	
	SEW 083
	StE 460 TM

	
	NFA 36-201
	E 460 R

	
	UNI 7382
	Fe E 460 KGTM

	
	BS 4360
	-

	
	ASTM
	A 572 Gr.65


S460M steel plate Chemical Composition 
 

	Grade
	C max
	Si max
	Mn max
	P max
	S max
	N max
	AL max
	Nb max
	V max
	Ti max
	Cr max
	Ni max
	Mo max
	Cu max
	CEV max

	S460M
	0.16%
	0.60%
	1.70%
	0.03%
	0.025%
	0.025%
	0.02%
	0.05%
	0.12%
	0.05%
	0.30%
	0.80%
	0.20%
	0.55%
	0.48%


S460M steel sheet Mechnical Properties 
 

	Temperature
	-10
	0
	20

	Notch impact test. Min. absorbed energy
	43
	47
	55


	Nominal thickness(mm)
	to 16
	16-40
	40-63
	63-80
	80-100
	100-120

	ReH-Minimun yield strength(Mpa)
	460
	440
	430
	410
	400
	385


	Nominal thickness(mm)
	to 40
	40-63
	63-80
	80-100
	100-120

	Rm-Tensile strength(Mpa)
	540-720
	530-710
	510-690
	500-680
	490-660

	Nominal thickness(mm)
	-

	A-Minimum elongation Lo=5,65√So(%)
	17


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


