[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

EN10113 S460ML steel plate/sheet,EN10113 S460ML steel plate/sheet, under EN standard, we can regard S460ML steel plate/sheet for Fine-grain structural steels, the rmomechanically rolled steel.
EN10113S460ML is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -50 degree.

	  S460ML EN 10113-3Number:1.8838
	Comparision of steel grades

	
	SEW 083
	TStE 460 TM

	
	NFA 36-201
	E 460 FP

	
	UNI 7382
	Fe E 460 KGTM

	
	BS 4360
	55 EE

	
	ASTM
	A 572 Gr.65


Chemical Composition 
 

	Grade
	C max
	Si max
	Mn max
	P max
	S max
	N max
	AL max
	Nb max
	V max
	Ti max
	Cr max
	Ni max
	Mo max
	Cu max
	CEV max

	S420ML
	0.16%
	0.60%
	1.70%
	0.025%
	0.02%
	0.025%
	0.02%
	0.05%
	0.12%
	0.05%
	0.30%
	0.80%
	0.20%
	0.55%
	0.48%



S460ML steel plate  Mechnical Properties 
 
	Temperature
	-50
	-40
	-30
	-20
	-10
	0
	20

	Notch impact test. Min. absorbed energy
	27
	31
	40
	47
	51
	55
	63


	Nominal thickness(mm)
	to 16
	16-40
	40-63
	63-80
	80-100
	100-120

	ReH-Minimun yield strength(Mpa)
	460
	440
	430
	410
	400
	385


	Nominal thickness(mm)
	to 40
	40-63
	63-80
	80-100
	100-120

	Rm-Tensile strength(Mpa)
	540-720
	530-710
	510-690
	500-680
	490-660

	Nominal thickness(mm)
	-

	A-Minimum elongation Lo=5,65√So(%)
	17


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


