[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

 S460N steelis a higher yield strength structural grade than S420N. In -20 degree impact test and normalized delivery station.
Commonly used in the engineering and construction industry, S460N offers high yield and tensile strengthand is supplied with a variety of treatments and test options making it a highly usable steel in your construction project.
BEBON steel has much experience in manufacture S460N, we do that according to EN10025-3 adopt standard. Our advantage is that we could supply steel plate in the fastest delivery time and in best quality, even in one plate in usual specification.

About S460N steel PLATEdetail information，please refer to technical date in following.

	S460N
 EN 10025-3
	Comparison of steel grades

	
	UNE36081
	AE460KG/AE460KW

	
	DIN17102
	STE460

	
	NFA 36-201
	E460R

	
	BS4036
	-

	
	UN
	FE E 460KG N



S460N steel PLATE  Chemical analysis -% by mass*

	Chemical elements
	C
max
	Si
 max
	Mn
 
	P
max
	S
max.
	Cu
max
	Cr
max
	Ni
max
	V
max
	Nb
max
	Al
min

	%,by mass
	0.20
	0.60
	1.00-1.70
	0.030
	0.025
	0.55
	0.30
	0.50
	0.12
	0.05
	0.02


S460N steel  Mechanical properties
	thickness
	Yield StrengthReH[N/mm2]
transv.min.
	TensileStrengthRm[N/mm2]transv.
	Fracture Elongation[%]transv. min.
	Notch Impact
Energy1)Ch Vcomplete samplelongitud. min [J]

	t≤ 16mm
t >16mm
	460
440
	 
	 
	         +20   KV 31J
           0   KV 27J
         -10    KV 24J
         -20    KV 20J
         -40    -
         -50    -

	   t < 3mm
  t≥ 3mm
	 
	540-720
	 
	

	Up to 1.5mm
1.51-2.00mm
2.01-2.50mm
2.51-2.99mm
 ≥ 3mm
	 
	 
	17
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


