[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

THE SG255 steel plateis characterised by a minimum yield strength of 245 - 355 MPa and by good weldability. The user of  SG255 steel grades must make sure that his calculation, design and processing methods are appropriate for the material. The SG255 steel grades of this series are used for manufacturing gas cylinders by welding cold-formed parts together and normalizing the finished cylinder.
JIS G 3116-2000

Steel sheet,plate and strip for gas cylinders
 SG255 hot steel Chemical composition        unit%
	Symbol
	 Chemical composition

	
	C
 max
	Si
max
	Mn
 max
	P
max
	S
max

	SG255
	0.20
	-
	0.30
	0.040
	0.040

	SG295
	0.20
	0.35
	1.00
	0.040
	0.040

	SG325
	0.20
	0.55
	1.50
	0.040
	0.040

	SG365
	0.20
	0.55
	1.50
	0.040
	0.040



 SG255 steel plate Mechanical properties 

	Symbol
	Yield point or proof stress
N/mm2 (min)
	Tensile strength
N/mm2 min
	Elongation % min
 
	Tensile test piece
	Bendability

	
	
	
	
	
	Bending
Angle
	Inside radius
	Test piece

	SG255
	255
	400
	26
	NO.5 in rolling direction
	180°
	Thickness x 1.0
	No.3 in rolling direction

	SG295
	295
	440
	26
	
	180°
	Thickness x 1.5
	

	SG325
	325
	490
	22
	
	180°
	
	

	SG365
	365
	540
	20
	
	180°
	
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


