[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

SM400/SM490 Hot rolled steel plate /sheet always be used in  the following field 
(1)SM400 Hot rolled steelused for metallurgical, mechanical, electrical construction field
(2)SM490 Hot rolled steel used for ships, military (armored) Construction
(3)SM400/SM490 steel plate /sheet used for outside engineering, machine tool base, automobile rear of products

JIS G 3106-1999
Rolled steels for welded structure
SM400 Hot rolled steel sheet  Chemical composition unit%
	Symbol
	 Chemical composition

	
	C
 max
	Si
max
	Mn
 
	P
max
	S
max

	SM400A
	0.23
	-
	2.5xc min
	0.035
	0.035

	SM400B
	0.20
	0.35
	0.6-1.40
	0.035
	0.035

	SM400C
	0.19
	0.35
	1.4 max
	0.035
	0.035

	SM490A
	0.20
	0.55
	1.6 max
	0.035
	0.035

	SM490B
	0.19
	0.55
	1.6 max
	0.035
	0.035

	SM490C
	0.19
	0.55
	1.6 max
	0.035
	0.035

	SM490YA
	0.20
	0.55
	1.6 max
	0.035
	0.035

	SM490YB
	0.20
	0.55
	1.6 max
	0.035
	0.035

	SM520B
	0.20
	0.55
	1.6 max
	0.035
	0.035

	SM520C
	0.20
	0.55
	1.6 max
	0.035
	0.035

	SM570
	0.19
	0.55
	1.6 max
	0.035
	0.035


SM400 Hot rolled steel plate   Mechanical properties
	Symbol
	Yield point or proof stress
N/mm2 (min)
	Tensile strength
N/mm2
	Elongation

	
	Thickness of steel mm
	Thickness of steel mm
	thinckness
	Test piece
	% min

	
	16 or under
	Over 16-40
	100 or under
	
	
	

	SM400A
SM400B
SM400C
	245
	235
	400-510
	<5
	NO.5
	23

	
	
	
	
	≥5 <16
	NO.1A
	19

	
	
	
	
	≥16 <50
	NO.1A
	22

	SM490A
SM490B
SM490C
	325
	315
	490-610
	<5
	NO.5
	22

	
	
	
	
	≥5 <16
	NO.1A
	17

	
	
	
	
	≥16 <50
	NO.1A
	21

	SM490YA
SM490YB
	365
	355
	490-610
	<5
	NO.5
	19

	
	
	
	
	≥5 <16
	NO.1A
	15

	
	
	
	
	≥16 <50
	NO.1A
	19

	SM520B
SM520C
	365
	355
	520-640
	<5
	NO.5
	19

	
	
	
	
	≥5 <16
	NO.1A
	15

	
	
	
	
	≥16 <50
	NO.1A
	19

	SM570
	460
	450
	570-720
	<5
	NO.5
	19

	
	
	
	
	≥5 <16
	NO.5
	26

	
	
	
	
	≥16 <50
	NO.5
	20

	Symbol of grade
	Test temperature °C
	Charp Absorption Energy J (min)
	Test piece

	SM400B
	0
	27
	No.4 in rolling direction

	SM400C
	0
	47
	

	SM490B
	0
	27
	

	SM490C
	0
	47
	

	SM490YB
	0
	27
	

	SM520B
	0
	27
	

	SM520C
	0
	47
	

	SM570
	-5
	47
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


