[image: image1.jpg]BEBON

BebonChina.com

3




Henan BEBON international co.,ltd.

Under JIS  G3131-1996 standard, MSPHC steel plate/sheet  Main Application:
Household applicance, metal decorating, tinplating, tubbing, building color coated.

JIS G 3131-1996 
Hot rolled Mild steel plates,sheets and strip
 SPHC steel Chemical composition  unit%
	Symbol
	 Chemical composition

	
	C
 max
	Mn
max
	P
max
	S
max

	SPHC
	0.15
	0.60
	0.050
	0.050

	SPHD
	0.10
	0.50
	0.040
	0.040

	SPHE
	0.10
	0.50
	0.030
	0.035



 SPHC steel  sheet Mechanical properties
	Symbol
	Tensile strength N/mm2 min
	Elongation% min
	Tensile test piece
	Bendability

	
	
	≥1.2 <1.6mm
	≥1.6 <2mm
	≥2
<2.5mm
	≥2.5
<3.2mm
	≥3.2
<4mm
	≥4mm
	
	Bending angle
	Inside Radius
	Test piece

	
	
	
	
	
	
	
	
	
	
	<3.2mm
	≥3.2
mm
	

	SPHC
	270
	27
	29
	29
	29
	31
	31
	No.5 in rolling direction
	180°
	Flat on itself
	Thickness x 0.5
	No.3 in rolling direction

	SPHD
	270
	30
	32
	33
	35
	33
	39
	
	-
	-
	-
	

	SPHE
	270
	31
	33
	35
	37
	39
	41
	
	-
	-
	-
	


[image: image2.jpg]


BEBON international —— We are specialized in hot rolled steel plate/coil.
Tel:0086-371-86151827 86151627                                E-mail:BB@Bebonchina.com                          
Fax: 0086-371-86011881                                        Web:http://www.bebonchina.com
Oficina Dir: 2801 B# Intermational enterise center Zhengzhou city in China.


